CHRONG YI CO., LTD.

STITCHED GLASS FIBER BINDER FREE MAT :

- Introduction

CYMAT is the glass mat produced in high quality glass fiber and stitched into fabric without any binder. The product is easily to wet-out and suitable for hand lay-up, vacuum bagging and also for vacuum injection and other RTM-process. The fabric is drapable, and conforms well to complex geometry components. Table 1. is the CYMAT products.

# Table 1. CYMAT Products

| Item | Thickness (mm) | *FAW (g/m2) |
| --- | --- | --- |
| CYMAT 225 | 0.28 | 225 |
| CYMAT 300 | 0.37 | 300 |
| CYMAT 450 | 0.55 | 450 |
| CYMAT 600 | 0.73 | 600 |
| CYMAT 900 | 1.10 | 900 |
| CYMAT 1200 | 1.46 | 1200 |

*Total weight of ±5% is acceptable。

- CYMAT Laminate Property

The fiber weight content could reach 45% in hand lay-up process. Table 2. is the laminate property of CYMAT.

Table 2. CYMAT Laminate Property

| CYMAT |  | Fiber Content |
| --- | --- | --- |
|  |  | (45% wt.) |
| Tensile Modulus | Gpa | 8.5 |
| Tensile Strength | Mpa | 130 |
| Breaking elongation | % | 1.35 |