| 1. PRODUCT NAME | DB 800-E |
| --- | --- |
| 2. COLOUR CODE | Blue |  |
| 3. TYPICAL APPLICATIONS |  |
| This biaxial product is suitable for hand lay-up, vacuum bagging of relatively flat components, and also for vacuum injection and other RTM-process. Ideal for shear load supporting components and laterally loaded panels with aspect ratio from 1 to 3. It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |
| 4. FABRIC SPECIFICATIONS |  |
| Layer orientation Degree [(] | 0 | +45 | 90 | -45 |  |
| Layer weight [g/m2] |  | 392 | 8 | 392 |  |
| Material |  | E-glass | E-glass | E-glass |  |
| Weight, knitting yarn | [g/m2] | : | 7 |  |
| Weight, total | [g/m2] | : | 799 ( 3 % |  |
| Standard roll width | [cm] | : | 126 |  |
| Standard roll length (approx.) | [m] | : | 70 |  |
| Standard roll weight (approx.) | [kg] | : | 70 |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |
| Matrix type | Fibre weight fraction | Fibre volume fraction | Layer thickness |
| Isophthalic polyester | 59.9[%] | 41.8 [%] | 0.75 [mm] |
| Mechanical property |  |  | 0( | +45( | 90( | -45( |
| Tensile modulus | ASTM D3039-76 | [GPa] | 10.5* | 18.9* | 10.5* | 18.9* |
| Compressive modulus | ASTM D695 | [GPa] | 10.5* | 18.9* | 10.5* | 18.9* |
| Tensile strength | ASTM D3039-76 | [MPa] | 127* | 441 | 127* | 409 |
| Compressive strength | ASTM D695 | [MPa] | 151* | 241* | 151* | 241* |
| Elongation at break | ASTM D3039-76 | [%] |  | 2.9 |  | 2.6 |
| Shear strength, inplane | ASTM 4255-83 | [MPa] | 136 | 66.2 | 136* | 66.2* |
| Shear strength, interlam | ASTM 2344-84 | [MPa] | 15.8 | 30.4 |  |  |
| Tensile strength out of plane | ASTM C297-61 | [MPa] | 26.0 |  |  |  |
| *Laminate Plate Theory calculations **Test results |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |
| Type approved by: | DNV |  |  |  |  |