| 1. PRODUCT NAME |  |  |  | DB 800-E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2. COLOUR CODE |  |  |  | Blue |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3. TYPICAL APPLICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| This biaxial product is suitable for hand lay-up, vacuum bagging of relatively flat components, and also for vacuum injection and other RTM-process. Ideal for shear load supporting components and laterally loaded panels with aspect ratio from 1 to 3. It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. FABRIC SPECIFICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Layer orientation Degree [] |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |  |  |  |  |  |  |
| Layer weight [g/m2] |  |  |  |  |  |  |  |  | 392 |  |  |  |  | 8 |  |  | 392 |  |  |  |  |  |  |  |
| Material |  |  |  |  |  |  |  |  | E-glass |  |  |  |  | E-glass |  |  | E-glass |  |  |  |  |  |  |  |
| Weight, knitting yarn |  |  | [g/m2] |  |  |  | : | 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weight, total |  |  | [g/m2] |  |  |  | : | 799  3 % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll width |  |  | [cm] |  |  |  | : | 126 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll length (approx.) |  |  | [m] |  |  |  | : | 70 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll weight (approx.) |  |  | [kg] |  |  |  | : | 70 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Matrix type | Fibre weight fraction |  |  |  | Fibre volume fraction |  |  |  |  |  |  |  |  |  |  |  |  |  | Layer thickness |  |  |  |  |  |
| Isophthalic polyester | 59.9[%] |  |  |  | 41.8 [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.75 [mm] |  |  |  |  |  |
| Mechanical property |  |  |  |  |  |  |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |
| Tensile modulus |  | ASTM D3039-76 |  |  |  | [GPa] |  |  |  | 10.5* |  |  |  |  | 18.9* |  |  |  |  | 10.5* |  |  | 18.9* |  |
| Compressive modulus |  | ASTM D695 |  |  |  | [GPa] |  |  |  | 10.5* |  |  |  |  | 18.9* |  |  |  |  | 10.5* |  |  | 18.9* |  |
| Tensile strength |  | ASTM D3039-76 |  |  |  | [MPa] |  |  |  | 127* |  |  |  |  | 441 |  |  |  |  | 127* |  |  | 409 |  |
| Compressive strength |  | ASTM D695 |  |  |  | [MPa] |  |  |  | 151* |  |  |  |  | 241* |  |  |  |  | 151* |  |  | 241* |  |
| Elongation at break |  | ASTM D3039-76 |  |  |  | [%] |  |  |  |  |  |  |  |  | 2.9 |  |  |  |  |  |  |  | 2.6 |  |
| Shear strength, inplane |  | ASTM 4255-83 |  |  |  | [MPa] |  |  |  | 136 |  |  |  |  | 66.2 |  |  |  |  | 136* |  |  | 66.2* |  |
| Shear strength, interlam |  | ASTM 2344-84 |  |  |  | [MPa] |  |  |  | 15.8 |  |  |  |  | 30.4 |  |  |  |  |  |  |  |  |  |
| Tensile strength out of plane |  | ASTM C297-61 |  |  |  | [MPa] |  |  |  | 26.0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type approved by: |  |  |  |  |  |  | DNV |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |