| 1. PRODUCT NAME | DBL 600-E |
| --- | --- |
| 2. COLOUR CODE | Red | Magenta |
| 3. TYPICAL APPLICATIONS |  |
| This triaxial product is suitable for hand lay-up and vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm). Suitable also for vacuum injection and other RTM-process. Ideal for laterally loaded panels with aspect ratio from 1.5 to (. It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |
| 4. FABRIC SPECIFICATIONS |  |
| Layer orientation Degree [(] | 0 | +45 | 90 | -45 |  |
| Layer weight [g/m2] | 295 | 148 |  | 148 |  |
| Material | E-glass | E-glass |  | E-glass |  |
| Weight, knitting yarn | [g/m2] | : | 12 |  |
| Weight, total | [g/m2] | : | 603 ( 3 % |  |
| Standard roll width | [cm] | : | 126 |  |
| Standard roll length (approx.) | [m] | : | 80 |  |
| Standard roll weight (approx.) | [kg] | : | 61 |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |
| Matrix type | Fibre weight fraction | Fibre volume fraction | Layer thickness |
| Isophthalic polyester | 55[%] | 36.5 [%] | 0.6 [mm] |
| Mechanical property |  |  | 0( | +45( | 90( | -45( |
| Tensile modulus | ASTM D3039-76 | [GPa] | 17.8* | 12.6* | 8.5* | 12.6* |
| Compressive modulus | ASTM D695 | [GPa] |  |  |  |  |
| Tensile strength | ASTM D3039-76 | [MPa] | 448* | 290* | 106* | 290* |
| Compressive strength | ASTM D695 | [MPa] | 255* | 181* | 128* | 181* |
| Elongation at break | ASTM D3039-76 | [%] |  |  |  |  |
| Shear strength, inplane | ASTM 4255-83 | [MPa] | 113* | 105* | 113* | 105* |
| Shear strength, interlam | ASTM 2344-84 | [MPa] |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |
| Type approved by: | DNV |  |  |  |  |