| 1. PRODUCT NAME | DBL 800-E |
| --- | --- |
| 2. COLOUR CODE | Magenta |  |
| 3. TYPICAL APPLICATIONS |  |
| This triaxial product is suitable for hand lay-up and vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm). Suitable also for vacuum injection and other RTM-process. Ideal for laterally loaded panels with aspect ratio from 1.5 to (. It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |
| 4. FABRIC SPECIFICATIONS |  |
| Layer orientation Degree [(] | 0 | +45 | 90 | -45 |  |
| Layer weight [g/m2] | 413 | 199 | 8 | 199 |  |
| Material | E-glass | E-glass | E-glass | E-glass |  |
| Weight, knitting yarn | [g/m2] | : | 10 |  |
| Weight, total | [g/m2] | : | 829 ( 3 % |  |
| Standard roll width | [cm] | : | 126 |  |
| Standard roll length (approx.) | [m] | : | 70 |  |
| Standard roll weight (approx.) | [kg] | : | 73 |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |
| Matrix type | Fibre weight fraction | Fibre volume fraction | Layer thickness |
| Isophthalic polyester | 53.7[%] | 35.6 [%] | 0.9 [mm] |
| Mechanical property |  |  | 0( | +45( | 90( | -45( |
| Tensile modulus | ISO 3268 | [GPa] | 20.3 | 14.6 | 9.9 | 14.1 |
| Compressive modulus | BS 2782 | [GPa] | 14.5 | 14.6 | 7.7 | 11.3 |
| Tensile strength | ISO 3268 | [MPa] | 404 | 199 | 104 | 190 |
| Compressive strength | BS 2782 | [MPa] | 293 | 211 | 144 | 219 |
| Elongation at break | ISO 3268 | [%] | 2.4 | 2.4 | 2.9 | 2.4 |
| Shear strength, inplane | ASTM 4255-83 | [MPa] | 96* | 107* | 78* | 107* |
| Shear strength, interlam | BS 2782 | [MPa] | 36.5 | 25.9 | 18.7 | 25.8 |
| *Laminate Plate Theory calculations **Test results |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |
| Type approved by: | DNV |  |  |  |  |