| 1. PRODUCT NAME |  |  |  | DBL 800-E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2. COLOUR CODE |  |  |  | Magenta |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3. TYPICAL APPLICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| This triaxial product is suitable for hand lay-up and vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm). Suitable also for vacuum injection and other RTM-process. Ideal for laterally loaded panels with aspect ratio from 1.5 to . It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. FABRIC SPECIFICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Layer orientation Degree [] |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |  |  |  |  |  |  |
| Layer weight [g/m2] |  |  |  | 413 |  |  |  |  | 199 |  |  |  |  | 8 |  |  | 199 |  |  |  |  |  |  |  |
| Material |  |  |  | E-glass |  |  |  |  | E-glass |  |  |  |  | E-glass |  |  | E-glass |  |  |  |  |  |  |  |
| Weight, knitting yarn |  |  | [g/m2] |  |  |  | : | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weight, total |  |  | [g/m2] |  |  |  | : | 829  3 % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll width |  |  | [cm] |  |  |  | : | 126 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll length (approx.) |  |  | [m] |  |  |  | : | 70 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll weight (approx.) |  |  | [kg] |  |  |  | : | 73 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Matrix type | Fibre weight fraction |  |  |  | Fibre volume fraction |  |  |  |  |  |  |  |  |  |  |  |  |  | Layer thickness |  |  |  |  |  |
| Isophthalic polyester | 53.7[%] |  |  |  | 35.6 [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.9 [mm] |  |  |  |  |  |
| Mechanical property |  |  |  |  |  |  |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |
| Tensile modulus |  | ISO 3268 |  |  |  | [GPa] |  |  |  | 20.3 |  |  |  |  | 14.6 |  |  |  |  | 9.9 |  |  | 14.1 |  |
| Compressive modulus |  | BS 2782 |  |  |  | [GPa] |  |  |  | 14.5 |  |  |  |  | 14.6 |  |  |  |  | 7.7 |  |  | 11.3 |  |
| Tensile strength |  | ISO 3268 |  |  |  | [MPa] |  |  |  | 404 |  |  |  |  | 199 |  |  |  |  | 104 |  |  | 190 |  |
| Compressive strength |  | BS 2782 |  |  |  | [MPa] |  |  |  | 293 |  |  |  |  | 211 |  |  |  |  | 144 |  |  | 219 |  |
| Elongation at break |  | ISO 3268 |  |  |  | [%] |  |  |  | 2.4 |  |  |  |  | 2.4 |  |  |  |  | 2.9 |  |  | 2.4 |  |
| Shear strength, inplane |  | ASTM 4255-83 |  |  |  | [MPa] |  |  |  | 96* |  |  |  |  | 107* |  |  |  |  | 78* |  |  | 107* |  |
| Shear strength, interlam |  | BS 2782 |  |  |  | [MPa] |  |  |  | 36.5 |  |  |  |  | 25.9 |  |  |  |  | 18.7 |  |  | 25.8 |  |
| *Laminate Plate Theory calculations **Test results |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type approved by: |  |  |  |  |  |  | DNV |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |