| 1. PRODUCT NAME | DBLT 1150-E |
| --- | --- |
| 2. COLOUR CODE | Orange | Black |
| 3. TYPICAL APPLICATIONS |  |
| This quadriaxial product is suitable for hand lay-up, vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm), vacuum injection and other RTM-process. Due to the fibre layers the resulting laminate will have quasi-isotropic properties and orientation is non-critical. It is very stable and easy to roll out, has good wet out properties, and fibre contents above 60% is easily obtained with ordinary hand lay-up. |
| 4. FABRIC SPECIFICATIONS |  |
| Layer orientation Degree [(] | 0 | +45 | 90 | -45 |  |
| Layer weight [g/m2] | 295 | 276 | 283 | 276 |  |
| Material | E-glass | E-glass | E-glass | E-glass |  |
| Weight, knitting yarn | [g/m2] | : | 11 |  |
| Weight, total | [g/m2] | : | 1141 ( 3 % |  |
| Standard roll width | [cm] | : | 126 |  |
| Standard roll length (approx.) | [m] | : | 50 |  |
| Standard roll weight (approx.) | [kg] | : | 72 |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |
| Matrix type | Fibre weight fraction | Fibre volume fraction | Layer thickness |
| Isophthalic polyester | 54[%] | 35.6 [%] | 1.3 [mm] |
| Mechanical property |  |  | 0( | +45( | 90( | -45( |
| Tensile modulus | ISO 3268 | [GPa] | 15.2 | 17.8 | 16.0 | 15.0 |
| Compressive modulus | BS 2782 | [GPa] | 11.5 | 11.3 | 11.5 | 11.3 |
| Tensile strength | ISO 3268 | [MPa] | 257 | 215 | 224 | 204 |
| Compressive strength | BS 2782 | [MPa] | 265 | 354 | 268 | 263 |
| Elongation at break | ISO 3268 | [%] | 2.5 | 2.1 | 2.2 | 2.2 |
| Shear strength, inplane | ASTM 4255-83 | [MPa] | 135* | 79* | 141* | 79* |
| Shear strength, interlam | BS 2782 | [MPa] | 36.8 | 27.4 | 30.4 | 31.1 |
| Tensile strength, out of plane | ASTM C297-61 | [MPa] |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |
| Type approved by: | DNV |  |  |  |  |