| 1. PRODUCT NAME |  |  |  | DBLT 600-E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2. COLOUR CODE |  |  |  | Magenta |  |  |  |  |  |  |  |  | Blue |  |  |  |  |  |  |  |  |  |  |  |
| 3. TYPICAL APPLICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| This quadriaxial product is suitable for hand lay-up, vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm), vacuum injection and other RTM-process. Due to the fibre layers the resulting laminate will have quasi-isotropic properties and orientation is non-critical. It is very stable and easy to roll out, has good wet out properties, and fibre contents above 60% is easily obtained with ordinary hand lay-up. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. FABRIC SPECIFICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Layer orientation Degree [] |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |  |  |  |  |  |  |
| Layer weight [g/m2] |  |  |  | 158 |  |  |  |  | 148 |  |  |  |  | 151 |  |  | 148 |  |  |  |  |  |  |  |
| Material |  |  |  | E-glass |  |  |  |  | E-glass |  |  |  |  | E-glass |  |  | E-glass |  |  |  |  |  |  |  |
| Weight, knitting yarn |  |  | [g/m2] |  |  |  | : | 11 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weight, total |  |  | [g/m2] |  |  |  | : | 616  3 % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll width |  |  | [cm] |  |  |  | : | 126 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll length (approx.) |  |  | [m] |  |  |  | : | 80 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll weight (approx.) |  |  | [kg] |  |  |  | : | 62 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Matrix type | Fibre weight fraction |  |  |  | Fibre volume fraction |  |  |  |  |  |  |  |  |  |  |  |  |  | Layer thickness |  |  |  |  |  |
| Isophthalic polyester | 55[%] |  |  |  | 36.5 [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.6 [mm] |  |  |  |  |  |
| Mechanical property |  |  |  |  |  |  |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |
| Tensile modulus |  | ASTM D3039-76 |  |  |  | [GPa] |  |  |  | 13.5* |  |  |  |  | 13.2* |  |  |  |  | 13.2* |  |  | 13.2* |  |
| Compressive modulus |  | ASTM D695 |  |  |  | [GPa] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Tensile strength |  | ASTM D3039-76 |  |  |  | [MPa] |  |  |  | 253* |  |  |  |  | 237* |  |  |  |  | 250* |  |  | 237* |  |
| Compressive strength |  | ASTM D695 |  |  |  | [MPa] |  |  |  | 195* |  |  |  |  | 191* |  |  |  |  | 192* |  |  | 191* |  |
| Elongation at break |  | ASTM D3039-76 |  |  |  | [%] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Shear strength, inplane |  | ASTM 4255-83 |  |  |  | [MPa] |  |  |  | 111* |  |  |  |  | 113* |  |  |  |  | 95* |  |  | 113* |  |
| Shear strength, out of plane |  | ASTM C297-61 |  |  |  | [MPa] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type approved by: |  |  |  |  |  |  | DNV |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |