| 1. PRODUCT NAME | DBT 800-E |
| --- | --- |
| 2. COLOUR CODE | Red |  |
| 3. TYPICAL APPLICATIONS |  |
| This triaxial product is suitable for hand lay-up and vacuum bagging of relatively flat components. (min. curvature radius approx. 15 mm). Suitable also for vacuum injection and other RTM-process. Ideal for laterally loaded panels with aspect ratio from 1.5 to (. It is very stable and easy to roll out. Fibre contents above 60% is easily obtained with ordinary hand lay-up. |
| 4. FABRIC SPECIFICATIONS |  |
| Layer orientation Degree [(] | 0 | +45 | 90 | -45 |  |
| Layer weight [g/m2] |  | 199 | 389 | 199 |  |
| Material |  | E-glass | E-glass | E-glass |  |
| Weight, knitting yarn | [g/m2] | : | 6 |  |
| Weight, total | [g/m2] | : | 793 ( 3 % |  |
| Standard roll width | [cm] | : | 126 |  |
| Standard roll length (approx.) | [m] | : | 70 |  |
| Standard roll weight (approx.) | [kg] | : | 70 |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |
| Matrix type | Fibre weight fraction | Fibre volume fraction | Layer thickness |
| Isophthalic polyester | 59.6[%] | 41.8 [%] | 0.75 [mm] |
| Mechanical property |  |  | 0( | +45( | 90( | -45( |
| Tensile modulus | ASTM D3039-76 | [GPa] | 9.9 | 14.5* | 19.3 | 14.5* |
| Compressive modulus | ASTM D695 | [GPa] | 9.9* | 14.5 * | 18.8 | 14.5* |
| Tensile strength | ASTM D3039-76 | [MPa] | 95 | 223* | 555 | 223* |
| Compressive strength | ASTM D695 | [MPa] | 131 | 185* | 299 | 185* |
| Elongation at break | ASTM D3039-76 | [%] | 2.7 |  | 3.4 |  |
| Shear strength, inplane | ASTM 4255-83 | [MPa] | 88* | 71* | 88* | 71* |
| Shear strength, interlam | ASTM 2344-84 | [MPa] |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |
| Type approved by: | DNV |  |  |  |  |