| 1. PRODUCT NAME |  |  |  | L 500-E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2. COLOUR CODE |  |  |  | Orange |  |  |  |  |  |  |  |  | Yellow |  |  |  |  |  |  |  |  |  |  |  |
| 3. TYPICAL APPLICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| This unidirectional product is suitable for hand lay-up, vacuum bagging of relatively flat component, vacuum injection and other RTM-process. Ideal for components with unidirectional loads, such as beam, flanges, etc. The product is easily cut in tapes to requested widths, in order to fit the application exactly. Fibre contents above 55% is easily obtained with ordinary hand lay-up. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. FABRIC SPECIFICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Layer orientation Degree [] |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |  |  |  |  |  |  |
| Layer weight [g/m2] |  |  |  | 472 |  |  |  |  |  |  |  |  |  | 45 |  |  |  |  |  |  |  |  |  |  |
| Material |  |  |  | E-glass |  |  |  |  |  |  |  |  |  | E-glass |  |  |  |  |  |  |  |  |  |  |
| Weight, knitting yarn |  |  | [g/m2] |  |  |  | : | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weight, total |  |  | [g/m2] |  |  |  | : | 527  3 % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll width |  |  | [cm] |  |  |  | : | 126 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll length (approx.) |  |  | [m] |  |  |  | : | 70 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll weight (approx.) |  |  | [kg] |  |  |  | : | 47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Matrix type | Fibre weight fraction |  |  |  | Fibre volume fraction |  |  |  |  |  |  |  |  |  |  |  |  |  | Layer thickness |  |  |  |  |  |
| Isophthalic polyester | 55.0 [%] |  |  |  | 36.51 [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.57 [mm] |  |  |  |  |  |
| Mechanical property |  |  |  |  |  |  |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |
| Tensile modulus |  | ASTM D3039-76 |  |  |  | [GPa] |  |  |  | 25.8** |  |  |  |  | 8.4* |  |  |  |  | 8.0* |  |  | 8.4* |  |
| Compressive modulus |  | ASTM D695 |  |  |  | [GPa] |  |  |  | 25.8** |  |  |  |  | 8.4* |  |  |  |  | 8.0* |  |  | 8.4* |  |
| Tensile strength |  | ASTM D3039-76 |  |  |  | [MPa] |  |  |  | 720** |  |  |  |  | 102* |  |  |  |  | 70* |  |  | 102* |  |
| Compressive strength |  | ASTM D695 |  |  |  | [MPa] |  |  |  | 351* |  |  |  |  | 143* |  |  |  |  | 122* |  |  | 143* |  |
| Elongation at break |  | ASTM D3039-76 |  |  |  | [%] |  |  |  | 2.9** |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Shear strength, inplane |  | ASTM 4255-83 |  |  |  | [MPa] |  |  |  | 63* |  |  |  |  | 115* |  |  |  |  | 63* |  |  | 115* |  |
| Shear strength, interlam |  | ASTM 2344-84 |  |  |  | [MPa] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type approved by: |  |  |  |  |  |  | DNV |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |