| 1. PRODUCT NAME |  |  |  | LT 600-E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2. COLOUR CODE |  |  |  | Red |  |  |  |  |  |  |  |  | Yellow |  |  |  |  |  |  |  |  |  |  |  |
| 3. TYPICAL APPLICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| This unidirectional product is suitable for hand lay-up, vacuum bagging of relatively flat component, vacuum injection and other RTM-process. Ideal for components with unidirectional loads, such as beam, flange, etc. The product is easily cut in tapes to requested widths, in order to fit the application exactly. Fibre contents above 55% is easily obtained with ordinary hand lay-up. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. FABRIC SPECIFICATIONS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Layer orientation Degree [] |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |  |  |  |  |  |  |
| Layer weight [g/m2] |  |  |  | 295 |  |  |  |  |  |  |  |  |  | 297 |  |  |  |  |  |  |  |  |  |  |
| Material |  |  |  | E-glass |  |  |  |  |  |  |  |  |  | E-glass |  |  |  |  |  |  |  |  |  |  |
| Weight, knitting yarn |  |  | [g/m2] |  |  |  | : | 14 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weight, total |  |  | [g/m2] |  |  |  | : | 606  3 % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll width |  |  | [cm] |  |  |  | : | 126 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll length (approx.) |  |  | [m] |  |  |  | : | 80 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Standard roll weight (approx.) |  |  | [kg] |  |  |  | : | 61 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. TYPICAL LAMINATE PROPERTIES |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Matrix type | Fibre weight fraction |  |  |  | Fibre volume fraction |  |  |  |  |  |  |  |  |  |  |  |  |  | Layer thickness |  |  |  |  |  |
| Isophthalic polyester | 52.0[%] |  |  |  | 34 [%] |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.7 [mm] |  |  |  |  |  |
| Mechanical property |  |  |  |  |  |  |  |  |  | 0 |  |  |  |  | +45 |  |  |  |  | 90 |  |  | -45 |  |
| Tensile modulus |  | ISO 3268 |  |  |  | [GPa] |  |  |  | 18.7 |  |  |  |  | 8.6* |  |  |  |  | 24.0 |  |  | 8.6* |  |
| Compressive modulus |  | BS 2782 |  |  |  | [GPa] |  |  |  | 14.4 |  |  |  |  |  |  |  |  |  | 14.1 |  |  |  |  |
| Tensile strength |  | ISO 3268 |  |  |  | [MPa] |  |  |  | 307 |  |  |  |  | 128* |  |  |  |  | 281 |  |  | 128* |  |
| Compressive strength |  | BS 2782 |  |  |  | [MPa] |  |  |  | 278 |  |  |  |  | 151 |  |  |  |  | 280 |  |  | 151 |  |
| Elongation at break |  |  |  |  |  | [%] |  |  |  | 2.3 |  |  |  |  |  |  |  |  |  | 1.8 |  |  |  |  |
| Shear strength, inplane |  | ASTM 4255-83 |  |  |  | [MPa] |  |  |  | 66* |  |  |  |  | 153* |  |  |  |  | 66* |  |  | 151* |  |
| Shear strength, interlam |  | BS 2782 |  |  |  | [MPa] |  |  |  | 34.4 |  |  |  |  |  |  |  |  |  | 29.6 |  |  |  |  |
| *Laminate Plate Theory calculations **Test results |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. QUALITY ASSURANCE AND TYPE APPROVAL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CYMAX reinforcements are made of certified materials only, and the production is in conformance with the International Quality system Standard ISO 9002. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Type approved by: |  |  |  |  |  |  | DNV |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |